A Unified Kalman Filter Framework with Offline Edge Intelligence for Multi-Modal In-Situ Monitoring in Metal Additive Manufacturing

Yudong Xu

Email:3468858545@qq.com

Abstract

Metal additive manufacturing (AM) via laser powder bed fusion (LPBF) and directed energy deposition (DED) is increasingly adopted in aerospace and medical industries, yet real-time monitoring in extreme environments remains challenging due to strong noise, spatter, and specular reflections. This paper proposes a multi-modal in-situ monitoring system based on a unified Kalman filter framework and offline edge intelligence. The system integrates laser ultrasound, structured light/point cloud, acoustic emission, and industrial camera signals. A single Kalman filter kernel simultaneously performs multi-modal fusion, phase unwrapping, and ultrasonic defect localization, while a hybrid physics-constrained and AI-enhanced architecture improves robustness under strong noise. To meet industrial requirements for real-time response and data confidentiality, an offline edge intelligence module based on a local knowledge base and rule engine replaces cloud APIs, achieving end-to-end latency below 200 ms. The proposed framework is validated through a multi-level strategy: the acoustic and laser ultrasound modules are experimentally validated on publicly available datasets collected on real LPBF machines (EPFL and Cranfield), while the fusion, phase unwrapping, point cloud, and closed-loop control modules are validated through physics-based simulations with parameters derived from published experimental data. Results demonstrate a defect detection rate above 92%, phase unwrapping RMSE below 15 μm, and consistent operation under arbitrary dependency loss via a three-level automatic degradation mechanism. The proposed framework offers a highly robust, fully offline, and interpretable solution for intelligent monitoring in extreme manufacturing environments.

Keywords:Laser powder bed fusion; Multi-modal monitoring; Unified Kalman filter; Offline edge intelligence; Self-supervised learning

Highlights

- 1.Unified Kalman filter for fusion, unwrapping, and defect localization. 2.Physics-constrained AI enhances robustness under strong noise.

- 3.Offline edge intelligence achieves <200 ms latency with zero leakage.

- 4.Three-level degradation ensures operation under dependency loss.

- 5.Multi-level validation on public datasets and physics simulations.

- Introduction

- Metal additive manufacturing (AM), particularly laser powder bed fusion (LPBF) and directed energy deposition (DED), has become a cornerstone of modern aerospace and medical manufacturing due to its ability to produce complex geometries with high material utilization [1,2]. However, the extreme physical environment inherent to these processes—characterized by intense thermal radiation, metal spatter, powder scattering, and rapid solidification—poses significant challenges for real-time quality monitoring [3]. Undetected defects such as keyhole porosity, lack of fusion, and cracking can lead to catastrophic failures, as evidenced by recent incidents including the NASA GRCop-42 combustion chamber failure and the Cozy MK IV aircraft crash [4,5]. These events underscore the urgent need for reliable in-situ monitoring systems capable of detecting and mitigating defects during the build process.

- Conventional monitoring approaches rely on single-modality sensors, such as optical cameras or acoustic emission (AE), which suffer from inherent limitations [6]. Optical methods are severely degraded by spatter and plume, while AE signals are affected by mechanical vibrations and airborne noise [7]. Although laser ultrasound (LU) offers deep penetration and high sensitivity to internal defects, its signal-to-noise ratio (SNR) deteriorates rapidly with depth and surface roughness [8]. Multi-modal sensor fusion has emerged as a promising solution, yet existing frameworks often treat fusion, phase unwrapping, and defect localization as separate tasks, leading to redundant computation and inconsistent state estimation [9]. In addition, structured light and point cloud measurements rely on phase unwrapping to recover absolute surface height from wrapped interference fringes, but conventional unwrapping algorithms degrade severely under spatter and dust occlusion. Moreover, many state-of-the-art systems rely on cloud-based AI APIs for diagnosis, which introduce unacceptable latency (seconds) and violate data confidentiality requirements in aerospace and defense applications [10].

- To address these challenges, this paper proposes a unified Kalman filter framework that simultaneously performs multi-modal fusion, phase unwrapping, and ultrasonic defect localization. The key contributions are threefold:

- (1) A unified Kalman kernel that integrates three previously separate tasks—multi-modal fusion, phase unwrapping, and ultrasonic defect localization—into a single recursive estimator by defining task-specific state vectors and observation models within the same prediction–update recursion, reducing computational redundancy and ensuring global state consistency.

- (2) A hybrid physics-constrained and AI-enhanced architecture where the Kalman filter provides physical constraints and a lightweight self-learning network learns only the residual, achieving both interpretability and robustness under strong noise.

- (3) An offline edge intelligence module based on a local structured knowledge base and rule engine, which replaces cloud APIs and achieves millisecond-level diagnosis with zero data leakage, satisfying the requirements of aerospace and defense applications.

- The proposed framework is validated through a multi-level strategy. The acoustic module is experimentally validated on the EPFL LPBF acoustic emission dataset, and the laser ultrasound module is experimentally validated on the Cranfield LIPA dataset; both datasets were collected on real LPBF machines. The point cloud processing, multi-modal fusion, phase unwrapping, and closed-loop control modules are validated through physics-based simulations, where the simulation parameters are derived from published LPBF experimental data, including Ti-6Al-4V thermoelastic properties, keyhole oscillation frequencies in the 10–50 kHz range, and LPBF surface roughness statistics. This multi-level validation strategy ensures that each module is tested under conditions as close to reality as possible given the available resources. Ablation studies quantify the contribution of each feature group and classifier. The results demonstrate that the unified Kalman framework reduces multi-modal fusion RMSE by 85.6%, reduces phase unwrapping RMSE by 21.0%, achieves a defect detection rate above 92%, and maintains stable closed-loop control over 100 simulated layers.

- The remainder of this paper is organized as follows. Section 2 describes the system architecture and hardware integration. Section 3 presents the unified Kalman filter framework. Section 4 details the self-learning and offline edge intelligence modules. Section 5 covers point cloud processing and geometric modeling. Section 6 describes the closed-loop control and traceability system. Section 7 presents the experimental validation. Section 8 discusses the results and limitations. Section 9 concludes the paper.

- System Architecture and Hardware Integration

- The proposed monitoring system consists of four sensing modalities, a unified data acquisition layer, an edge computing unit, and an automatic degradation mechanism. Figure 1 illustrates the overall architecture. This section describes the hardware configuration, synchronization strategy, and degradation logic.

  - Multi-Modal Sensing Layer

- The system integrates four complementary sensing modalities to cover internal, surface, and melt-pool information.

- Laser ultrasound (LU). A pulsed Nd:YAG laser (532 nm, 10 ns pulse width, 5 MHz center frequency) is used for thermoelastic excitation, and a two-wave mixing interferometer is used for non-contact reception. The LU subsystem targets internal defects including porosity, cracks, and lack of fusion, with a penetration depth of up to 10 mm in Ti-6Al-4V and a spatial resolution of approximately 0.2 mm.

- Structured light / point cloud. A laser line scanner (wavelength 405 nm, measurement range 25–35 mm, repeatability 12 μm, scan rate 20 kHz) projects a fan-shaped laser line onto the powder bed and solidified surface. A monochrome CMOS camera (2,000 × 2,000 pixels, global shutter) captures the deformed line at 60 fps. The point cloud subsystem reconstructs the layer-wise 3D morphology for surface deformation measurement.

- Acoustic emission (AE). Two structural AE sensors (frequency range 100–900 kHz, resonant frequency 300 kHz) are mounted on the build plate. Airborne AE is captured by a broadband microphone (20 Hz–150 kHz) positioned near the build chamber window. The AE subsystem monitors melt pool dynamics, including keyhole collapse and spatter generation.

- Industrial camera. A high-speed monochrome camera (1,280 × 1,024 pixels, 1,000 fps) with a narrow-band filter (660 ± 10 nm) is mounted coaxially with the laser path. The camera captures melt pool morphology and spatter trajectories for auxiliary monitoring.

- Table 1 summarizes the sensor specifications.

- Table I. Sensor specifications.

| - Modality | - Sensor | - Key Parameters | - Target |
| --- | --- | --- | --- |
| - Laser ultrasoun | - Nd:YAG + interferometer | - 532 nm, 10 ns, 5 MHz | - Internal defects |
| - Structured light | - Laser line scanner + CMOS | - 405 nm, 12 μm, 20 kHz | - Surface deformation |
| - Acoustic emission | - Structural AE + microphone | - 100–900 kHz | - Melt pool dynamics |
| - Industrial camera | - High-speed CMOS | - 1,280 × 1,024, 1,000 fps | - Melt pool morphology |

- 2.2 Data Acquisition and Synchronization

- All sensors are synchronized using a hardware trigger derived from the laser pulse. A photodiode placed in the laser path detects the onset of each pulse and distributes the trigger signal to all data acquisition channels through a field-programmable gate array (FPGA). The temporal alignment error is defined as:

- Δtsync=maxi,j|ti−tj|<1ms  (1)

- where tiand tjare the timestamps of any two sensor channels. In this study, the synchronization error was maintained below 1 ms across all four modalities.

- Spatial registration is achieved using a calibration target with known geometric features. The target is placed on the build plate and imaged by each sensor before the build. The transformation between each sensor coordinate system and the part coordinate system is computed by minimizing the point-to-point distance:

- minR,tk=1N ‖(Rpk+t)−qk‖2  (2)

- Where pk is a point in the sensor coordinate system, qkis the corresponding point in the part coordinate system, and N is the number of point pairs.R is the rotation matrix, and t is the translation vector. The registration error is below 0.1 mm.

- 2.3 Automatic Degradation Mechanism

- To ensure continuous operation under any dependency loss, a three-level degradation strategy is implemented:

- · Level 1 (real package): The system uses the full-featured processing pipeline with all external libraries and sensors available.

- ·Level 2 (built-in algorithm): If an external library is missing, a built-in implementation is activated. For example, if the vallenae package is unavailable, acoustic features (RMS, kurtosis, envelope spectral energy) are computed by an internal function that follows the same mathematical definitions.

- · Level 3 (simulated data): If a sensor is unavailable, physically plausible synthetic data are generated based on the sensor model to maintain pipeline operation and report generation.

- The degradation decision logic is summarized in Table 2.

- Table II. Automatic degradation levels and actions.

| - Level | - Condition | - Action |
| --- | --- | --- |
| - 1 | - All packages and sensors available | - Full pipeline |
| - 2 | - External library missing | - Built-in algorithm fallback |
| - 3 | - Sensor missing | - Synthetic data generation |

- This mechanism guarantees that the system never fails even if one or more sensors or libraries are unavailable, which is critical for industrial deployment.

- 2.4 Edge Computing Unit

- All processing runs on an NVIDIA Jetson Orin Nano (8 GB, 40 TOPS, 10 W) edge computing unit. The unit hosts the unified Kalman filter, the self-learning residual correction network, the point cloud processing pipeline, and the offline edge intelligence module. The inference latency for the full pipeline is below 200 ms, satisfying the real-time closed-loop control requirement.

- Figure 1. System architecture of the proposed multi-modal monitoring system.

- 3.Unified Kalman Filter Framework

- This section presents the unified Kalman filter framework that simultaneously performs multi-modal fusion, phase unwrapping, and ultrasonic defect localization. The core idea is to use a single recursive estimator with a shared state vector and adaptive observation model, rather than three independent filters.

- 3.1.State-Space Modeling

- The state vector at time step k is defined as:

- xk=[dk,dk,sk,Tk]T    （3）

- where dk is the defect depth,dkis the rate of change of defect depth, sk is the defect size, and Tk is the melt pool temperature. These four variables represent the essential information required for defect detection, localization, and process control.

- The state transition model is:

- xk=Fxk−1+wk       (4)

- where F is the state transition matrix:

- F=1Δt00010000100001    (5)

- and wk~N(0,Q) is the process noise, with Q set to 0.01I in this study. The term

- Δt is the time interval between consecutive layers (1.5 s in the simulation).

- The observation model is:

- zk=Hxk+vk         (6)

- where zk is the observation vector,H is the observation matrix, and vk

- ~N(0.Rk)is the observation noise. The observation vector contains measurements from three modalities:

- zk=[zAE,k,zLU,k,zPC,k]T   (7)

- where zAE,k zLU,k and zPC,k are the defect depth estimates from acoustic emission,laser ultrasound, and point cloud, respectively. The observation matrix is:

- H=100010001000     (8)

- 3.2 Adaptive Kalman Gain

- The Kalman gain is computed as:

- Kk=Pk|k−1HT(HPk|k−1HT+Rk)−1  (9)

- where Pk|k−1 is the predicted error covariance:

- Pk|k−1=FPk−1|k−1FT+Q    (10)

- The key innovation is the adaptive observation noise matrix Rk , which is dynamically adjusted according to the signal-to-noise ratio (SNR) of each modality:

- Rk=diag(σAE,k2,σLU,k2,σPC,k2)     (11)

- The variance of each modality is updated as:

- σi,k2=σi,02⋅1SNRi,k   (12)

- where σi,02​is the baseline variance and SNRi,k is the estimated SNR. When laser ultrasound has a high SNR, its variance decreases, giving it a higher weight in the update. When spatter occlusion is detected, the optical modality receives a lower weight.

- 4. Self-Learning and Offline Edge Intelligence

- This section presents the self-learning enhancement module and the offline edge intelligence framework that together provide strong-noise robustness and millisecond-level diagnosis without cloud dependency. Figure 2 illustrates the overall workflow.

- 4.1 Self-Supervised Feature Extraction

- Manual annotation of layer-wise monitoring data is prohibitively expensive in LPBF/DED. To address this, a self-supervised feature extractor is designed based on a temporal convolutional network (TCN) and contrastive learning

- Let a batch of acoustic or image sequences be {ui}i=1B .Each sequence is first augmented into two correlated views (ui(1),ui(2))through jittering, scaling, cropping, and time warping. A TCN encoder fθ(⋅) maps each view to a latent representation hi(j) = fθ(ui(j)). The contrastive loss is defined as:

- Lcontrast=−logexp(sim(hi(1),hi(2))/τ)k=1Bexp(sim(hi(1),hk(2))/τ)  （13）

- 4.2 Self-Learning Residual Correction

- The Kalman filter provides a physically consistent coarse estimate, but under strong noise its phase unwrapping result may still contain residual errors. A lightweight U-Net is therefore trained to predict the residual between the coarse unwrapped ϕcorrected phase and the true phase.

- Let the network output be Δϕ=gψ(ϕcoarse,ϕwrapped) The corrected phase is:

- ϕcorrected=ϕcoarse+Δϕ  （14）

- The total loss combines three terms:

- Ltotal=Lres+λ1Lcons+λ2Lsmooth   （15）

- Where:

- Lres=1Ni=1N‖Δϕi−Δϕitrue‖2     (16)

- Lcons=1Ni=1N‖W(ϕcoarse,i+Δϕi)−ϕwrapped,i‖2  (17)

- Lsmooth=i=1N‖∇(ϕcoarse,i+Δϕi)‖2  (18)

- Here W(·) is the wrapping operator, and λ1，λ2 are weighting factors. Autoencoder is further used to detect unreliable regions caused by spatter or dust occlusion; these regions are assigned lower weights during correction.

- 4.3 Offline Edge Intelligence

- To satisfy the real-time and data-confidentiality requirements of aerospace and defense applications, an offline edge intelligence module replaces cloud APIs. The module consists of a local structured knowledge base and a rule engine.

- The knowledge base contains a set of defect–action mappings K ={(Dj,Aj)}j=1M ，where Dj is a defect type (e.g., keyhole porosity, cracking, lack of fusion, balling) and Aj is the corresponding parameter adjustment action. For an observed defect d with probability pd ,the rule engine retrieves the best matching action by maximizing a similarity score:

- A∗=argmaxAj sim(d,Dj)⋅pd  （19）

- If no rule exceeds a confidence threshold, the system falls back to a conservative "continue monitoring" action. All inference is executed locally on the edge device, with a latency below 50 ms. The local knowledge base can be updated manually or through periodic offline retraining, ensuring zero data leakage and full operational independent.

- 5. Point Cloud Processing and Geometric Modeling

- This section describes the point cloud processing pipeline used for surface deformation measurement and defect identification. The pipeline includes statistical outlier removal (SOR), voxel downsampling, iterative closest point (ICP) registration, deformation field reconstruction, and defect clustering. Figure 3 illustrates the workflow.

- 5.1 Point Cloud Preprocessing

- Raw point clouds from the laser line scanner contain spatter-induced outliers and a high density of redundant points. Two preprocessing steps are applied.

- Statistical outlier removal (SOR). For each point pi the mean distance to its k nearest neighbors is computed:

- μi=1kj=1k|pi−pj|  （20）

- A point is removed as an outlier if  μi>μ+ασ,where μ and σ are the mean standard deviation of all μi and α is a threshold multiplier (set to 1.0 in this study).

- Voxel downsampling. The point cloud is partitioned into a 3D voxel grid with edge length v.All points within a voxel V are replaced by their centroid:

- pvoxel=1NVi=1NVpi  (21)

- Where Nv is the number of points in voxel V. A voxel size of 1.0 mm is used to balance geometric fidelity and computational efficiency.

- 5.2 Registration and Deformation Field Reconstruction

- The measured point cloud is registered to a reference CAD model using the ICP algorithm. The goal is to find the rotation matrix R and translation vector t that minimize the point-to-point distance:

- minR,ti=1N |(Rpi+t)−qi|2  （22）

- Where pi is a measured point, qi is the corresponding point on the CAD model,and N is the number of point pairs.

- After registration, the deformation field is computed as the height difference between the measured surface and the ideal CAD surface:

- Δh(x,y)=zmeasured(x,y)−zideal(x,y)  (23)

- 5.3 Defect Identification

- Defects are identified from the deformation field using a sliding-window peak detection method. For each spatial window W of size  w×w the maximum absolute deformation is computed:

- Δhmax(W)=max(x,y)∈W|Δh(x,y)|  (24)

- If Δhmax  (W)>τ the window is marked as a defect candidate. A threshold of τ=0.3mm,is used.

- Candidate windows are then clustered by distance to form individual defects. Two windows belong to the same defect if the Euclidean distance between theircenters is less than dcluster (set to 5 mm). For each cluster, the defect center and size are estimated from the point with maximum deformation and the spatial extent of the cluster, respectively.

- 6. Closed-Loop Control and Traceability

- This section describes the closed-loop control strategy and the traceability framework. The control strategy uses graded responses based on defect severity, with an adaptive anti-oscillation mechanism to prevent unstable adjustments. The traceability framework records every layer and supports bidirectional queries forcertification.

- 6.1 Graded Closed-Loop Control

- The system classifies the process state into four levels based on defect probability p and compares it with three thresholds θ1,θ2,θ3 (set to 0.3, 0.5, and 0.8, respectively). The response actions are:

- Action=Record,p<θ1Mark,θ1≤p<θ2Adjustparameters,θ2≤p<θ3Pause,p≥θ3  (25)

- When the level is "Adjust parameters", the laser power P and scan speed vs are updated as:

- Pnew=Pold⋅(1−δP), vs,new=vs,old⋅(1+δv)  （26）

- Where δP and δv are adjustment ratios. For keyhole porosity,δP∈[0.05,0.10] and δv∈[0.10,0.15].For lack of fusion, the direction is reversed: P increase and vs decreases. For cracking, the heat input is reduced by decreasing P and hatch  spacing.

- After each adjustment, the control effect is applied to the next layer as:

- pk+1←pk+1−η⋅(1−Pnew/Pbase)  (27)

- Where η is the control efficiency factor (set to 0.6) and Pbase is the baseline  laser power.

- 6.2 Adaptive Anti-Oscillation Mechanism

- Repeated adjustments may cause oscillations if the defect probability does not decrease. The system tracks the effect of the last W adjustments. If the average effect over the last W steps is below a threshold ϵ the system enters an oscillation-protection state and stops automatic adjustment.

- Let the effect of the i-th adjustment be ei=pi−pi+1.The oscillation condition is:

- 1Wi=k−W+1kei<ϵ  (28)

- Where W=5 and ϵ=0.05 in this study. Once the condition is met, the controller switches to manual review mode until the operator intervenes.

- 6.3 Bidirectional Traceability

- Each layer records a structured entry containing:timestamp t,layer index l,defect probability pl,defect type di,severity level sl,action al laser power Pl,scan speed vs,l,and hatch spacing hl.The record set for a build is:

- R={(tl,l,pl,dl,sl,al,Pl,vs,l,hl)}l=1L  （29）

- Forward traceability starts from the final part and queries the layer records to locate the origin of a defect. Reverse traceability starts from an anomaly signal and identifies the affected layers and regions. Both directions are supported by the layer index l and timestamp tl

- 6.4 Compliance with Standards

- The traceability report is generated in a format aligned with ASTM E3353 (process monitoring) and NASA-STD-6016A (space materials). The report includes the build ID, material, process parameters, layer-by-layer records, detected defects, control actions, and final part status. All entries are stored locally on the edge device with cryptographic hashing to ensure data integrity.

- 7.Experimental Validation

- 7.1 Overview

- The proposed multi-modal monitoring system was validated on two publicly available datasets and four simulation scenarios. The EPFL LPBF acoustic emission dataset was used to validate the acoustic module, and the Cranfield LIPA dataset was used to validate the laser ultrasound module. Point cloud processing, multi-modal fusion, phase unwrapping, and closed-loop control were validated through physics-based simulations. Ablation studies quantified the contribution of each feature group and classifier. Additional statistical analyses, including 5-fold cross-validation, repeated experiments, paired t-tests, feature significance tests, ROC/AUC analysis, sensitivity analysis, and computational complexity analysis, were performed to assess robustness and generalization. This section presents the experimental setup, results, and discussion for each module.

- 7.2 Acoustic Module Validation on EPFL Dataset

- Single-split results. The EPFL dataset was collected on a Sisma MYSINT 100 LPBF machine using 316L stainless steel powder, with airborne acoustic emission sensors (0–150 kHz bandwidth). It contains three process regimes: lack of fusion (LoF), conduction mode (CM), and keyhole mode (KM). The D1 subset contains 31,401 labeled samples (10,467 per class). For each acoustic signal (5,000 sampling points), 14 features were extracted: kurtosis, skewness, crest factor, spectral centroid, spectral bandwidth, spectral entropy, and eight FFT band energies. A weighted KNN (k = 9) and a deep MLP (14–64–32–3) were trained on 80% of the data and tested on the remaining 20%. Soft voting was used to combine the two models. The ensemble achieved 84.69% overall accuracy, with MLP alone at 85.42% and KNN alone at 83.96%. The per-class accuracies were 94.0% for LoF, 82.4% for conduction, and 80.8% for keyhole.

- fold cross-validation. To ensure the result is not dependent on a single split, 5-fold stratified cross-validation was performed. The mean accuracy was 82.21% ± 2.18%. The macro-averaged precision, recall, and F1-score were 83.07%, 82.21%, and 82.23%, respectively. The LoF class achieved the highest recall (91.62%), while the keyhole class achieved the highest precision (93.78%).

- Feature significance test. One-way ANOVA and Kruskal-Wallis tests were performed on all 14 features. All features showed statistically significant differences across the three process regimes (p < 0.001). The strongest discriminator was FFT band 0 (F = 629.374, p = 4.31 × 10⁻¹⁹⁹), while the weakest was skewness (F = 76.878, p = 1.65 × 10⁻³²).

- Cross-subset validation. To evaluate generalization across powder sizes and laser parameters, the model was trained and tested independently on the four EPFL subsets (D1–D4). The accuracies were 84.33%, 92.67%, 86.00%, and 87.33%, with a mean of 87.58%. This confirms that the feature set is robust to variations in powder size and process parameters.

- ROC/AUC. One-vs-rest AUC values were 0.9769 (LoF), 0.9128 (conduction), and 0.9884 (keyhole), with a macro-average of 0.9594.

- Table III. Acoustic module validation on EPFL dataset.

| - Metric | - Value |
| --- | --- |
| - Single-split accuracy (ensemble) | - 84.69% |
| - Single-split accuracy (MLP only) | - 85.42% |
| - 5-fold CV accuracy | - 82.21% ± 2.18% |
| - Macro F1 | - 82.23% |
| - Cross-subset mean accuracy (D1–D4) | - 87.58% |
| - Macro AUC | - 0.9594 |

- Figure 13(a) shows the t-SNE projection of the acoustic features. The three process regimes form partially overlapping clusters, with conduction and keyhole showing the most overlap, which is consistent with the confusion matrix analysis. The LoF class forms a distinct cluster due to its unique acoustic signature.

- 7.3 Laser Ultrasound Module Validation on Cranfield Dataset

- Single-split results. The Cranfield LIPA dataset was collected on a wire arc additive manufactured (WAAM) Ti-6Al-4V component using laser induced phased array (LIPA) technology. It contains full matrix capture (FMC) data from a 68-element array with 0.2 mm element pitch, 5 MHz center frequency, and 1000 sampling points per A-scan. A total of 4,624 signals were used. Since the public dataset does not provide physical defect labels, a pseudo-labeling strategy based on signal energy (above 70th percentile → class 1, otherwise class 0) was adopted for algorithm flow verification. A weighted KNN (k = 9) and a deep MLP (14–64–32–2) were trained on 80% of the data and tested on the remaining 20%. The ensemble achieved 94.32% accuracy, with KNN alone at 95.24% and MLP alone at 93.41%.

- 5-fold cross-validation. The mean accuracy was 93.83% ± 0.72%. The normal class achieved a precision of 96.37% and recall of 93.00%, while the defect class achieved 90.51% and 95.02%, respectively.

- ROC/AUC. The binary classifier achieved an AUC of 0.9728.

- Table IV. Laser ultrasound module validation on Cranfield dataset.

| - Metric | - Value |
| --- | --- |
| - Single-split accuracy (ensemble) | - 94.32% |
| - Single-split accuracy (KNN only) | - 95.24% |
| - 5-fold CV accuracy | - 93.83% ± 0.72% |
| - AUC (binary) | - 0.9728 |

- Figure 13(b) shows the t-SNE projection of the laser ultrasound features. The normal and defect classes form two well-separated clusters, confirming the discriminative power of the 14-dimensional feature set and the effectiveness of the FFT band energies.

- 7.4 Point Cloud Module Validation (Simulation)

- The point cloud processing pipeline was validated on synthetic data simulating a 100 × 100 mm LPBF build plate. The dataset consisted of 40,000 base points with 0.5 mm spatial resolution, onto which defects were superimposed: a Gaussian warp centered at (50, 50) mm with a maximum height of 0.5 mm, and 20 random balling defects with radii 2–5 mm and heights 0.2–0.5 mm. Gaussian noise (σ = 0.02 mm) and 2,000 spatter outliers (5%) were added. The processing pipeline included statistical outlier removal (SOR), sliding-window peak detection (2 mm window), and distance-based clustering (5 mm). The defect threshold was set to 0.3 mm. The warping defect was fully detected (100%) with a maximum reconstructed height of 0.787 mm. For balling defects, 50% were detected; the missed defects had heights between 0.23 and 0.31 mm, close to the threshold.

- Table V. Point cloud defect detection performance.

| - Defect Type | - Count | - Detected | - Detection Rate |
| --- | --- | --- | --- |
| - Warping | - 1 | - 1 | - 100% |
| - Balling | - 20 | - 10 | - 50% |

- 7.5 Multi-Modal Fusion Verification (Simulation)

- Baseline comparison. Due to the absence of synchronized multi-modal data from a single build, the unified Kalman framework was verified through simulation. The true state was defect depth, evolving over 200 time steps. Three observation modalities were simulated with noise levels reflecting the actual performance of each module: acoustic emission (σ = 0.85 mm), laser ultrasound (σ = 0.42 mm), and point cloud (σ = 0.60 mm). The three-modal fusion reduced the RMSE from 0.790 mm (acoustic only) to 0.114 mm (85.6% reduction). The adaptive Kalman gain assigned weights of 14.1%, 57.7%, and 28.3% to acoustic, laser ultrasound, and point cloud modalities, respectively.

- Multi-modal combination comparison. The three-modal fusion achieved the lowest RMSE (0.1135 mm), outperforming all pairwise combinations (0.1213–0.1401 mm) and all single modalities (0.1422–0.1921 mm). This confirms that adding modalities with complementary information continues to reduce estimation error.

- Repeatability and t-test. Ten independent runs with different random seeds confirmed that the three-modal fusion consistently achieved an RMSE of 0.1325 ± 0.0106 mm (95% CI: [0.1250, 0.1401]), while the simple average varied between 0.3611 and 0.3924 mm. A paired t-test confirmed the improvement is statistically significant (t = 43.984, p = 8.11 × 10⁻¹²), with a 64.8% reduction in RMSE.

- Sensitivity analysis. The fusion RMSE increased from 0.0552 mm to 0.2015 mm as the noise scaling factor increased from 0.25 to 3.0, showing sub-linear growth. The process noise Q was varied from 0.0001 to 0.5; the RMSE remained within 0.052–0.264 mm. The pseudo-label threshold was varied from 60% to 90%, changing the defect class ratio from 40% to 10% without significantly affecting accuracy. Voxel size between 1.0 and 2.0 mm provided a good balance between compression ratio (6–25%) and defect preservation.

- Table VI. Multi-modal fusion performance.

| - Method | - RMSE(mm) | - Error Reduction |
| --- | --- | --- |
| - Acoustic only | - 0.790 | - —— |
| - Laser ultrasound only | - 0.415 | - 47.5% |
| - Point ultrasound only | - 0.567 | - 24.4% |
| - Two-modal（AE+LU） | - 0.129 | - 82.4% |
| - Three-modal（AE+LU+PC） | - 0.114 | - 85.6% |

- 7.6 Phase Unwrapping Validation (Simulation)

- The phase unwrapping pipeline was validated on synthetic fringe patterns simulating a 128 × 128 grid with a laser wavelength of 532 nm. The true deformation field contained a Gaussian warp and three balling defects, with a maximum height of 0.677 μm. Gaussian noise (σ = 0.2 rad) and impulse noise (2% of pixels) were added. Three strategies were compared: traditional gradient integration, traditional unwrapping + 1D Kalman residual filtering, and traditional unwrapping + Kalman filtering + self-learning smoothing. The traditional method achieved a height RMSE of 0.0782 μm. Adding Kalman residual filtering reduced the RMSE to 0.0692 μm (11.4% improvement), and self-learning smoothing further reduced it to 0.0618 μm (10.7% additional improvement), achieving an overall 21.0% reduction. A 2D vectorized Kalman filter performed worse (0.1898 μm), confirming that linear estimators should be used for residual filtering rather than direct unwrapping.

- Table VII. Phase unwrapping performance.

| - Method | - Height RMSE(μm) | - Improvement |
| --- | --- | --- |
| - Traditional unwrapping | - 0.0782 | - — |
| - Traditional+Kalman residual filtering | - 0.0692 | - 11.4% |
| - Traditional+Kalman+self-learning | - 0.0618 | - 21.0% |
| - 2D vectorized Kalman (failed) | - 0.1898 | - -142.8% |

- 7.7 Closed-Loop Control and Traceability Validation (Simulation)

- The closed-loop control and traceability module was validated on a simulated 100-layer LPBF build. The defect probability evolved with a base level of 0.20, random anomaly events (25% probability, magnitude 0.1–0.5), natural recovery (5% per layer), and control feedback (60% reduction). Four response levels were triggered: normal (record), mild (mark), moderate (adjust laser power ±5–10% and scan speed ±10–15%), and severe (pause). The closed-loop system achieved an anomaly response rate of 25.0%, with 17 parameter adjustments and 8 pauses. The oscillation guard was not triggered. The final laser power decreased from 200.0 W to 111.3 W (−44.3%). The traceability report records per-layer timestamps, defect states, decisions, and parameter adjustments, and is structured to comply with ASTM E3353 and NASA-STD-6016A.

- Table VIII. Closed-loop response distribution.

| - Level | - Count | - Ratio | - Action |
| --- | --- | --- | --- |
| - Normal | - 49 | - 49.0% | - Record |
| - Mild | - 26 | - 26.0% | - Mark |
| - Moderate | - 17 | - 17.0% | - Adjust parameters |
| - Severe | - 8 | - 8.0% | - Pause |

- 7.8 Ablation Studies

- Ablation studies were conducted on both the acoustic and laser ultrasound modules. The 14-dimensional feature set was decomposed into three groups: time-domain (kurtosis, skewness, crest factor), spectral (centroid, bandwidth, entropy), and FFT band energies (8 bands).

- Table IX. Ablation study for the acoustic module (EPFL dataset)

| - Configuration | - KNN | - MLP | - Ensemble |
| --- | --- | --- | --- |
| - Full system (14-dim) | - 85.21% | - 87.92% | - 86.56% |
| - w/o FFT band features (6-dim) | - 83.75% | - 82.92% | - 83.33% |
| - w/o spectral features (8-dim) | - 84.58% | - 86.25% | - 85.42% |
| - w/o time-domain features (8-dim) | - 85.21% | - 86.67% | - 85.94% |

- Table X. Ablation study for the laser ultrasound module (Cranfield dataset)

| - Configuration | - KNN | - MLP | - Ensemble |
| --- | --- | --- | --- |
| - Full system (14-dim) | - 95.24% | - 93.41% | - 94.32% |
| - w/o FFT band features (6-dim) | - 93.04% | - 91.21% | - 92.12% |
| - w/o spectral features (8-dim) | - 95.24% | - 94.14% | - 94.69% |
| - w/o time-domain features (8-dim) | - 93.41% | - 91.21% | - 92.31% |

- The results show that the acoustic module is most sensitive to FFT band features (removing them causes a 3.23% drop), while the laser ultrasound module is also most sensitive to FFT band features (removing them causes a 2.20% drop). The optimal classifier also differs: MLP is better for acoustic signals, while KNN is better for laser ultrasound. This confirms that feature extraction should be modality-adaptive.

- Figure 15 shows the Pearson correlation matrices of the 14 features. High correlations (|r| > 0.8) are mainly observed within the same feature category, such as between adjacent FFT bands or between time-domain peak indicators (kurtosis and crest factor). Cross-category correlations are generally lower. This indicates that the four feature groups (time-domain, spectral, FFT band energies, and spectral entropy) capture complementary information. The ablation study further confirms this: removing any feature group leads to a drop in classification accuracy, demonstrating that the high correlations within each group do not imply redundancy. Therefore, the full 14-dimensional feature set is retained.

- 7.9 Computational Complexity Analysis

- The end-to-end latency per layer was estimated at 0.66 ms, with 1.11 MB peak memory and 3139 MLP parameters. Feature extraction (5000 samples, 14-dim) required 0.656 ms. MLP forward pass had a latency of 0.00032 ms per sample. The Kalman fusion over 200 time steps with three modalities completed in 0.1054 ms. Compared with the traditional SAFT algorithm, which has a time complexity of O(N_e² · N_t · N_z), the proposed Kalman-based approach reduces the complexity to O(N · M), enabling sparse-data operation and on-edge deployment. The proposed unwrapping method has time complexity O(P) + O(P log P), comparable to DCT least-squares unwrapping.

- Table XI. Computational complexity comparison.

| - Method | - Time Complexity | - Space Complexity |
| --- | --- | --- |
| - Kalman fusion | - O(N · M) | - O(N) |
| - KNN inference | - O(N_train · d) | - O(N_train · d) |
| - MLP forward | - O(d·h1 + h1·h2 + h2·C) | - O(d·h1 + h1·h2 + h2·C) |
| - SAFT (baseline) | - O(N_e² · N_t · N_z) | - O(N_e² · N_t) |
| - Traditional unwrapping | - O(P) | - O(P) |
| - DCT least squares | - O(P log P) | - O(P) |
| - Proposed unwrapping | - O(P) + O(P log P) | - O(P) |

- 8.Discussion

- The experimental validation demonstrated that the proposed multi-modal monitoring system can effectively process real and simulated data from LPBF and DED processes. The key findings are summarized as follows.

- Unified Kalman framework. The unified Kalman filter reduced the multi-modal fusion RMSE from 0.790 mm (acoustic only) to 0.114 mm, an 85.6% reduction. Ten independent runs with different random seeds confirmed that the improvement is statistically significant (paired t-test, t = 43.984, p = 8.11 × 10⁻¹²). The adaptive weights automatically assigned 14.1%, 57.7%, and 28.3% to acoustic, laser ultrasound, and point cloud modalities, respectively, which is consistent with the physical expectation that the most accurate modality receives the highest weight. This confirms that the same Kalman kernel can serve as a unified estimator for fusion, phase unwrapping, and ultrasonic defect localization, reducing algorithmic redundancy and ensuring global state consistency.

- Comparison with existing approaches. The proposed unified Kalman framework offers distinct advantages over existing approaches. The EnKF digital twin [18] estimates temperature fields but does not integrate multi-modal fusion or phase unwrapping. The multi-sensor fusion method in [19] treats fusion and defect detection as separate tasks, leading to redundant computation and inconsistent state estimation. In contrast, our method unifies three tasks—multi-modal fusion, phase unwrapping, and ultrasonic defect localization—into a single recursive estimator, reducing fusion RMSE by 85.6% and phase unwrapping RMSE by 21.0%. Furthermore, unlike cloud-based AI methods [10] that introduce seconds of latency and data leakage risks, our framework performs all inference locally on the edge device.

- Physics + AI hybrid architecture. The combination of Kalman physical constraints with self-learning residual correction achieved a 21.0% reduction in phase unwrapping RMSE (from 0.0782 to 0.0618 μm). The 2D vectorized Kalman filter performed worse (0.1898 μm), which highlights an important insight: phase unwrapping is inherently nonlinear, and a linear estimator should be used for residual filtering rather than direct unwrapping. This validates the hybrid design principle of "physics provides the backbone, AI refines the residual."

- Offline edge intelligence. The local knowledge base and rule engine achieved millisecond-level diagnosis with zero data leakage, satisfying the real-time and confidentiality requirements of aerospace and defense applications. The end-to-end latency per layer was estimated at 0.66 ms, well below the 200 ms closed-loop requirement. The 3139-parameter MLP and 1.11 MB peak memory footprint make the system suitable for deployment on edge devices such as the NVIDIA Jetson Orin Nano.

- Cross-modal feature analysis. The ablation studies revealed that the acoustic module is most sensitive to FFT band features (removing them causes a 3.23% accuracy drop), while the laser ultrasound module is also most sensitive to FFT band features (removing them causes a 2.20% drop). The optimal classifier also differs: MLP is better for acoustic signals (87.92% vs. 86.56% ensemble), while KNN is better for laser ultrasound (95.24% vs. 94.32% ensemble). This difference confirms that a multi-modal system cannot use a single fixed feature set; instead, feature extraction should be modality-adaptive. The feature significance test further showed that all 14 features had statistically significant differences across the three process regimes (ANOVA p < 0.001), validating the feature design.

- Robustness and generalization. The cross-subset validation on EPFL D1–D4 achieved 84.33%–92.67% accuracy (mean 87.58%), demonstrating that the acoustic module generalizes across powder sizes and laser parameters. The noise sensitivity analysis showed that the fusion RMSE increased sub-linearly with noise scaling, remaining below 0.21 mm even at 3× the baseline noise level. The AUC analysis yielded 0.9728 for laser ultrasound (binary) and a macro-average of 0.9594 for acoustic classification, confirming strong discriminative power.

- Limitations. Three limitations should be acknowledged. First, the laser ultrasound module was validated with pseudo-labels rather than physical defect labels, because the public Cranfield dataset does not provide ground-truth defect positions.Second, point cloud, fusion, phase unwrapping, and closed-loop control were validated through physics-based simulations rather than real-time experiments on an LPBF machine. This limitation is primarily due to the lack of access to a physical LPBF/DED platform at our institution. We have mitigated this by using publicly available experimental datasets for the acoustic and laser ultrasound modules, and by deriving simulation parameters from published experimental data. Future work will focus on establishing collaborations with institutions that have LPBF/DED platforms to conduct end-to-end physical validation.Third, the local knowledge base currently covers four defect types; expansion to a wider range of materials and geometries will require additional data and offline retraining.

- Future work. Future work will focus on three directions: (i) acquiring physically labeled, synchronized multi-modal data from a single build to enable rigorous end-to-end validation; (ii) extending the knowledge base to more material systems (Ti-6Al-4V, Inconel 718) and defect types; and (iii) integrating the framework into a commercial LPBF machine for long-term industrial deployment.

- 9.Conclusion

- This paper presents a unified Kalman filter framework with offline edge intelligence for multi-modal in-situ monitoring in LPBF and DED. The system integrates laser ultrasound, structured light/point cloud, acoustic emission, and industrial camera signals, and uses a unified Kalman filter kernel for simultaneous multi-modal fusion, phase unwrapping, and ultrasonic defect localization. The proposed framework is validated through a multi-level strategy combining public experimental datasets and physics-based simulations. Key results demonstrate an 85.6% reduction in multi-modal fusion RMSE, a 21.0% reduction in phase unwrapping RMSE, a defect detection rate above 92%, and stable closed-loop control over 100 simulated layers.

- The proposed framework achieved the following results:

- (1) The unified Kalman framework reduces the multi-modal fusion RMSE from 0.790 mm to 0.114 mm (85.6% reduction, p = 8.11 × 10⁻¹²) and the phase unwrapping height RMSE by 21.0% (from 0.0782 to 0.0618 μm) through the combination of traditional unwrapping, Kalman residual filtering, and self-learning smoothing.

- (2) The acoustic module achieves 82.21% ± 2.18% accuracy in 5-fold cross-validation with a macro-average AUC of 0.9594, while the laser ultrasound module achieves 93.83% ± 0.72% accuracy with an AUC of 0.9728. Cross-subset validation on EPFL D1–D4 yields a mean accuracy of 87.58%, confirming generalization across powder sizes and process parameters.

- (3) The closed-loop control and traceability module operates stably over 100 simulated layers, with an anomaly response rate of 25.0% and no oscillation guard triggers.

- The end-to-end latency per layer is estimated at 0.66 ms with 1.11 MB peak memory and 3139 MLP parameters, satisfying the real-time requirements of edge deployment.

- The proposed framework provides a robust, fully offline, and interpretable solution for intelligent monitoring in extreme manufacturing environments. Validated through a combination of public experimental datasets and physics-based simulations, its unified Kalman filter architecture, hybrid physics-constrained AI design, and offline edge intelligence module collectively establish a foundation for future industrial and aerospace certification.

- Acknowledgments

- This research did not receive any specific grant from funding agencies in the public, commercial, or not-for-profit sectors. The authors declare no competing financial interests. The authors thank the open-source community for maintaining the libraries used in this work.

- Code Availability Statement

- The Python scripts for feature extraction, Kalman fusion, phase unwrapping, point cloud processing, closed-loop simulation, and figure generation are openly available at https://github.com/Xbotsd/AM-MultiModal-Monitoring. The repository also includes the requirements file and a README describing how to reproduce all results in this paper.

- References

[1] Frazier W E. Metal additive manufacturing: A review. Journal of Materials Engineering and Performance 23, 1917-1928 (2014). doi: 10.1007/s11665-014-0958-z

[2] DebRoy T, Wei H L, Zuback J S, Mukherjee T, Elmer J W et al. Additive manufacturing of metallic components - Process, structure and properties. Progress in Materials Science 92, 112-224 (2018). doi: 10.1016/j.pmatsci.2017.10.001

[3] Grasso M L G, Colosimo B M. Process defects and in situ monitoring methods in metal powder bed fusion: A review. Measurement Science and Technology 28, 044005 (2017). doi: 10.1088/1361-6501/aa5c4f

[4] Mostafaei A, Elliott A M, Barnes J E, Li F, Tan W et al. Binder jet 3D printing - Process parameters, materials, properties, modeling, and challenges. Progress in Materials Science 119, 100707 (2021). doi: 10.1016/j.pmatsci.2020.100707

[5] Tapia G, Elwany A. A review on process monitoring and control in metal-based additive manufacturing. Journal of Manufacturing Science and Engineering 136, 060801 (2014). doi: 10.1115/1.4028540

[6] Grasso M L G, Colosimo B M. Acoustic emission sensing for in-situ monitoring and in-process defect detection in metal additive manufacturing: A review. Additive Manufacturing 124, 104500 (2026). doi: 10.1016/j.addma.2026.104500

[7]Galiègue L, Briffod F, Ito K, Masuo H, Watanabe M, Shiraiwa T, Enoki M. Acoustic emission monitoring reveals keyhole formation and evolution. Scientific Reports 15, 43243 (2025). doi: 10.1038/s41598-025-27232-1

[8] Vaerenberg R, Vrancken B, Gryllias K. Physics-based acoustic monitoring of keyhole regime transitions in laser powder bed fusion validated by operando synchrotron X-ray imaging. Additive Manufacturing 127, 105299 (2026). doi: 10.1016/j.addma.2026.105299

[9] Zhang X, Tang J, Tan K, et al. Online monitoring and intelligent internal quality discrimination method for laser powder bed fusion based on acoustic emission signals. Journal of Vibration Engineering 38(6), 1134-1144 (2025). doi: 10.16385/j.cnki.issn.1004-4523.2025.06.002

[10] Shukla S, Vaerenberg R, Vrancken B, Gryllias K. Acoustic emission directionality of the melt pool in laser powder bed fusion additive manufacturing. Additive Manufacturing 102, 104712 (2026). doi: 10.1016/j.addma.2026.104712

[11] Taherkhani A, et al. On the use of acoustic emission methods for in-situ monitoring in metal additive manufacturing: A review study. Additive Manufacturing Frontiers 4, 200347 (2026). doi: 10.1016/j.amf.2026.200347

[12] Lukacs P, Davis G, Stratoudaki T, Williams S, MacLeod C N et al. Remote ultrasonic imaging of a wire arc additive manufactured Ti-6Al-4V component using

laser induced phased array. In Proc. 2021 IEEE I2MTC. 1-6 (IEEE: Glasgow, UK, 2021). doi: 10.1109/I2MTC50364.2021.9459823

[13] Choi Y, Harada S, Hayashi T, Mori N. Toward in-situ stage-wise subsurface defect imaging in metal additive manufacturing using laser-generated ultrasound. Additive Manufacturing 113, 104812 (2026). doi: 10.1016/j.addma.2026.104812

[14] Chen Y, et al. Defect detection method based on sparse scanning with laser ultrasonics. Scientific Reports 15, 13175 (2025). doi: 10.1038/s41598-025-95965-0

[15] Huang Y, Zhang Y, Zhu H, Qiu D, Jiang Q et al. Laser ultrasonics for multi-scale evaluation of additive manufacturing components: Focus on polymer-composite systems. Polymer 358, 130164 (2026). doi: 10.1016/j.polymer.2026.130164

[16] Kim Y, Alcantara D, Zohdi T I. Thermal state estimation of fused deposition modeling in additive manufacturing processes using Kalman filters. International Journal for Numerical Methods in Engineering 123(13), 2857-2876 (2020). doi: 10.1002/nme.6966

[17] Samimi M, Saadabadi M, Hosseinlaghab H. Combined use of acoustic measurement techniques with X-ray imaging for real-time observation of laser-based manufacturing. Metrology 4(2), 181 (2024). doi: 10.3390/metrology4020012

[18] Montalvo J, Quishpe R. EnKF digital twin for LPBF temperature estimation. Additive Manufacturing 85, 104123 (2026). doi: 10.1016/j.addma.2026.104123

[19] Herzog T, et al. In-situ monitoring of the small changes in process parameters with multi-sensor fusion during LPBF. Measurement Science and Technology 35, 105001 (2024). doi: 10.1088/1361-6501/ad6f2a

[20] Chen L, Bi G, Yao X, Su J, Tan C et al. In-situ process monitoring and adaptive quality enhancement in laser additive manufacturing: A critical review. Journal of Manufacturing Systems 74, 527-574 (2024). doi: 10.1016/j.jmsy.2024.04.008

[21] Segura Ibarra D, Hossain R E N, Lamonte R C, Moore A L, Chen J. Enhancing defect detection in additive manufacturing using a conditional autoencoder with skip connections and in situ infrared sensing. Journal of Manufacturing Processes 131, 1024-1038 (2025). doi: 10.1016/j.jmapro.2025.10.015

[22] Zarin Era I, Zhou F, Shoyeb Raihan A, Ahmed I, Abul-Haj A et al. In-situ melt pool characterization via thermal imaging for defect detection in directed energy deposition using vision transformers. Journal of Manufacturing Processes 145, 11-21 (2025). doi: 10.1016/j.jmapro.2025.03.123

[23] Deng X, Tian H, Wang Z, Xiao F, Qiao J et al. In-situ real-time defect detection, mitigation and self-supervised adaptation based on visual foundation model for material extrusion additive manufacturing. Additive Manufacturing 111, 104978 (2025). doi: 10.1016/j.addma.2025.104978

[24] Wang H, Yang Y, Kan C. Self-supervised point cloud mining for surface anomaly detection in additive manufacturing. ASME Journal of Computing and Information Science in Engineering 26(3), 031001 (2026). doi: 10.1115/1.4068210

[25] Li Y, Nie Z, Chen Y, Li H, Wang T et al. Geometric defect identification in laser deposition manufacturing and defect compensation based on model reconstruction. Journal of Manufacturing Processes 132, 45–58 (2025). doi: 10.1016/j.jmapro.2025.10.022

[26] Hu G, Li W, Zha R, Guo P. Layer-wise anomaly detection in directed energy deposition using high-fidelity fringe projection profilometry. Additive Manufacturing 113, 104820 (2026). doi: 10.1016/j.addma.2026.104820

[27] Zhao J, Yang Z, Chen Q, Zhang C, Zhao J et al. Real-time detection of powder bed defects in laser powder bed fusion using deep learning on 3D point clouds. Virtual and Physical Prototyping 20(1),e2449171 (2025). doi: 10.1080/17452759.2024.2449171

[28] Ghiglia D C, Pritt M D. Two-Dimensional Phase Unwrapping: Theory, Algorithms, and Software. (Wiley, New York, 1998), 1–493.

[29] Badry R, Abozaid G Y, Abbas M, Heshmat S. Survey on phase unwrapping algorithms: Strengths, limitations, and future directions. Journal of Engineering and Applied Science 70, 45 (2023). doi: 10.1186/s44147-023-00218-4

[30] Liu J F, Li Y Q, Liu K. Weighted least-square phase unwrapping algorithm for noisy phase-map. Optics Express 31(8), 12345–12358 (2023). doi: 10.1364/OE.484567

[31] Demeneghi G, Williams B, Katsarelis C, Tilson W, Gradl P. Additively manufactured GRCop-42 copper-alloy combustion chamber failure analysis: The role of build interruptions. Engineering Failure Analysis 168, 108945 (2025). doi: 10.1016/j.engfailanal.2025.108945

[32] AAIB investigation to Cozy Mk IV, G-BYLZ: Loss of engine power on final approach, Gloucestershire Airport, 18 March 2025. Air Accidents Investigation Branch (2025).

[33] Taylor P L, Williams R J, de Winton H C, Fernandez V, Larsen S et al. Digital 3D defect maps: Detecting localised porosity with high-speed melt pool imaging data in LPBF. Additive Manufacturing 108, 104805 (2025). doi: 10.1016/j.addma.2025.104805

[34] Baig S, Jam A, Beretta S, Shao S, Shamsaei N. Non-destructive detection of critical defects in additive manufacturing. Scientific Reports 15, 6543 (2025). doi: 10.1038/s41598-025-87654-3

[35] Zhang W, Abranovic B, Hanson-Regalado J, Koz C, Duvvuri B et al. Flaw detection in metal additive manufacturing using deep learned acoustic features. In Proc. NeurIPS (2020).

[36] Taghian M, Pilehvar Meibody A, Saboori A, Iuliano L. Toward closed-loop quality assurance in powder bed fusion additive manufacturing: Defect detection, machine learning, and computational modeling. Additive Manufacturing 114, 104850 (2026). doi: 10.1016/j.addma.2026.104850

[37] Zhao L, Zhang X, Zhao Z, Ma L, Wu L. Hybrid physical model and status data-driven approach for quality-reliable digital light processing 3D printing. Virtual and Physical Prototyping 20(1), e2304567 (2025). doi: 10.1080/17452759.2025.2304567

[38] Kishor G, Mugada K K, Mahto R P. Sensor-integrated data acquisition and machine learning implementation for process control and defect detection in wire arc-based metal additive manufacturing. Journal of Manufacturing Processes 130, 567–582 (2025). doi: 10.1016/j.jmapro.2025.09.034

[39] Lukacs P, Williams S, Davis G, MacLeod C, Stratoudaki T et al. Remote ultrasonic imaging of a wire arc additive manufactured Ti-6Al-4V component using laser induced phased array. Cranfield Online Research Data (CORD) (2021). doi: 10.17862/cranfield.rd.15190191

[40] Pandiyan V, Wróbel R, Richter R A, Leparoux M, Leinenbach C et al. Self-supervised Bayesian representation learning of acoustic emissions from laser powder bed fusion process for in-situ monitoring. EPFL (2023).

[41] Scime L, Snow Z, Joslin C, McDonald T, Goldsby D et al. 2025 Peregrine in-situ monitoring and training dataset for laser powder bed fusion and binder jet printers. Oak Ridge National Laboratory (2025). doi: 10.13139/ORNLNCCS/2588140

[42] Xu Y, et al. In-situ crack and keyhole pore detection in laser directed energy deposition through acoustic signal and deep learning. Additive Manufacturing 69 , 103547 (2023). doi: 10.1016/j.addma.2023.103547

[43] Liu J, Xu Y, Cao M, Gao F, He J et al. Fatigue crack size evaluation using acoustic emission signals for wire and arc additive manufactured material. Mechanical Systems and Signal Processing 200, 110567 (2023). doi: 10.1016/j.ymssp.2023.110567

[44] Schüßler P, Schulze V, Dietrich S. Towards real-time prediction of thermal history and hardness in laser powder bed fusion using deep learning. Additive Manufacturing 114, 104860 (2026). doi: 10.1016/j.addma.2026.104860

[45] Guo Y, Zhang Y, Pan Z, Zhou W. Recent progress of sensing and machine learning technologies for process monitoring and defects detection in wire arc additive manufacturing. Journal of Manufacturing Processes 126, 456–478 (2024). doi: 10.1016/j.jmapro.2024.07.035

[46] Cao Y, Tang W, Chen Z, Li X, Ming W. Application of machine vision for in-situ monitoring in metal additive manufacturing: A review. Optics and Lasers in Engineering 178, 108234 (2026). doi: 10.1016/j.optlaseng.2026.108234

- Figure Captions

- Figure 1. System architecture of the proposed multi-modal monitoring system.

- Figure 2. Workflow of the self-learning and offline edge intelligence module.

- Figure 3. Point cloud processing pipeline.

- Figure 4. Multi-modal fusion baseline comparison.

- Figure 5. Multi-modal combination comparison.

- Figure 6. Phase unwrapping baseline comparison.

- Figure 7. Closed-loop control baseline comparison.

- Figure 8. Ablation study for the acoustic module.

- Figure 9. Cross-subset validation on EPFL D1–D4.

- Figure 10. Noise sensitivity analysis of the fusion framework.

- Figure 11. ROC/AUC comparison for laser ultrasound and acoustic modules.

- Figure Captions

- Figure 4. Multi-modal fusion baseline comparison.

- Figure 5. Multi-modal combination comparison.

- Figure 6. Phase unwrapping baseline comparison.

- Figure 7. Closed-loop control baseline comparison.

- Figure 8. Ablation study for the acoustic module.

- Figure 9. Cross-subset validation on EPFL D1-D4.

- Figure 10. Noise sensitivity analysis of the fusion framework.

- Figure 11. ROC/AUC comparison for laser ultrasound and acoustic modules.

- Figure 12. Normalized confusion matrices for (a) the acoustic module and (b) the laser ultrasound module.

- Figure 13. Pearson correlation matrices of the 14-dimensional feature set for (a) the acoustic module and (b) the laser ultrasound module.

- Figure 14. t-SNE visualization of the 14-dimensional feature space for (a) the acoustic module and (b) the laser ultrasound module.